## Slide 1
Tail-unsaturation Enables Fine-tuning on the Rheology of Sugar-based Surfactants
Jia-Fei Poon

## Slide 2
Surfactants
Compounds that lowers the surface
tension between two phases
Structure
Consist of a hydrophilic head group and
hydrophobic tail
Applications
Pharmaceutics, cosmetics,
detergents etc
Pharmaceutics
Detergent
Cosmetic products
H2O

## Slide 3
Surfactants:
Further Exploration
To link the physical properties with
the chemical architecture
Background and Aims
Sugar-based Surfactants:
A Greener Option
Minimized impact on aquatic
Environment
Not dependent on fossil-based
raw materials
Non-toxic
01
Sustainable
02
Safe
03
Ecosystem
Non-Newtonian rheology
04
Rheology
03
Fossil-
based
versus
01
Sugar-based
head group
02
Aliphatic
tail
Renewable
Renewable
BAC
LAS

## Slide 4
Non-Newtonian Fluid
The viscosity changes upon applied
force (e.g. syrup, ketchup)
The viscosity has a linear response
to the shear rate (e.g. water)
Worm-like
micelle
Decreased
Viscosity
01
Initial
state
03
Shear-
thinning
02
More
liquid-like
Viscosity
Shear rate
04
Worm-like
micelle

## Slide 5
=
=
Previous study:
α-anomer
β-anomer
Background and Aims
Sugar-based Surfactants:
A Greener Option
Not dependent on fossil-based
raw materials
01
Sustainable
Non-Newtonian rheology
04
Rheology
SANS:
Minimized impact on aquatic
Environment
Biodegradable
02
Stability
03
Ecosystem

## Slide 6
=
=
Previous study:
α-anomer
β-anomer
Background and Aims
Sugar-based Surfactants:
A Greener Option
Not dependent on fossil-based
raw materials
01
Sustainable
Non-Newtonian rheology
04
Rheology
=
This study:
To fine-tune the rheology
with unsaturation
05
Objective
Minimized impact on aquatic
Environment
Biodegradable
02
Stability
03
Ecosystem

## Slide 7
Library of sugar-based surfactants
To link the physical properties
with the chemical architecture
Synthesis of sugar-based
surfactants
01
Synthesis
Self-assembly
02
Properties
Rheology
03
Properties
G3-9-cis

## Slide 8
Self-assembly
To link the physical properties
with the chemical architecture
Synthesis of sugar-based
surfactants
01
Synthesis
Self-assembly
02
Properties
Rheology
03
Properties
Surfactant
Critical
micelle
conc.

## Slide 9
Linear rheology
To link the physical properties
with the chemical architecture
Synthesis of sugar-based
surfactants
01
Synthesis
Self-assembly
02
Properties
Rheology
03
Properties
Zero-shear
viscosity
Rotational
movement
Critical
Shear-rate
To probe the Non-Newtonian rheological behaviour of WLM

## Slide 10
Linear rheology
To link the physical properties
with the chemical architecture
Synthesis of sugar-based
surfactants
01
Synthesis
Self-assembly
02
Properties
Rheology
03
Properties
Shear-thinning
Influenced by
1) position
2) configuration of unsaturation
3) type of unsaturation
4) anomeric configuration
A broad range of zero-shear viscosity

## Slide 11
Linear rheology
To link the physical properties
with the chemical architecture
Synthesis of sugar-based
surfactants
01
Synthesis
Self-assembly
02
Properties
Rheology
03
Properties
Influenced by
1) position
2) configuration of unsaturation
3) type of unsaturation
4) anomeric configuration
Shear-thinning
A broad range of zero-shear viscosity

## Slide 12
Linear rheology
To link the physical properties
with the chemical architecture
Synthesis of sugar-based
surfactants
01
Synthesis
Self-assembly
02
Properties
Rheology
03
Properties
Influenced by
1) position
2) configuration of unsaturation
3) type of unsaturation
4) anomeric configuration
Shear-thinning
A broad range of zero-shear viscosity

## Slide 13
Linear rheology
To link the physical properties
with the chemical architecture
Synthesis of sugar-based
surfactants
01
Synthesis
Self-assembly
02
Properties
Rheology
03
Properties
Influenced by
1) position
2) configuration of unsaturation
3) type of unsaturation
4) anomeric configuration
Shear-thinning
A broad range of zero-shear viscosity

## Slide 14
Oscillatory Rheology
Viscoelastic properties
Materials exhibit both viscous and elastic properties upon deformation
G’ (●) = storage module; G” (○) = loss module
solid-like at high oscillation frequency
liquid-like at low oscillation frequency
01
Properties
02
Regiochem.
03
Stereochem.
04
alkyne
G’
Elastic
G”
Viscous
01
Intersection
= Relaxation time (τ)
Type of unsaturation: alkene > alkyne
The position of the unsaturation matters:
11-cis > 9-cis > 6-cis
Configuration of unsaturation: trans > cis

## Slide 15
Oscillatory Rheology
Viscoelastic properties
Materials exhibit both viscous and elastic properties upon deformation
01
Properties
03
Stereochem.
6-cis
τ = 268 s
9-cis
τ = 294 s
11-cis
τ = 900 s
04
alkyne
Type of unsaturation: alkene > alkyne
The position of the unsaturation matters:
11-cis > 9-cis > 6-cis
02
Regiochem.
G’ (●) = storage module; G” (○) = loss module
solid-like at high oscillation frequency
liquid-like at low oscillation frequency
Configuration of unsaturation: trans > cis

## Slide 16
Oscillatory Rheology
Viscoelastic properties
Materials exhibit both viscous and elastic properties upon deformation
01
Properties
02
Regiochem.
9-trans
τ = 1100 s
9-cis
τ = 294 s
9-alkyne
τ = 8 s
α-9-cis
τ = 6 s
Configuration of unsaturation: trans > cis
Type of unsaturation: alkene > alkyne
The position of the unsaturation matters:
11-cis > 9-cis > 6-cis
04
alkyne
03
Stereochem.
G’ (●) = storage module; G” (○) = loss module
solid-like at high oscillation frequency
liquid-like at low oscillation frequency

## Slide 17
Structural Information
SANS, SAXS and SLS
The rheology profile is not associated to the diameter, but the contour
and persistence length of the WLM
Worm-like micelle
Cylindrical, elongated and entangled system
L
03
Contour
length
02
Persistence
length
01
Diameter
Contour
length
Persistence
length

## Slide 18
Structural Information
Effect of Unsaturation
Contour (L) and persistence length (lp) are influenced by the configuration, position and types of unsaturation
Structure-Property Relationship
The longer the contour length, the more viscous the WLM
R2 = 0.96
R2 = 0.98

## Slide 19
Sugar-based
Surfactants
Self-assembly to
Worm-like Micelle
Tail-
Unsaturation
Rheology
Structure-Property
Relationship

## Slide 20
Marie Wahlgren
Adrian Sanchez-Fernandez
Najet Mahmoudi
Stefan Ulvenlund
Alessandro Gulotta

## Slide 21
Thank YOU