## Slide 1: Effect of the polymer conformation on the structure of protein - single chain nanoparticles
Thu Phuong Le1, Leide Cavalcanti2, Juan Colmenero1,3, Josetxo Pomposo1,4, Arantxa Arbe1 and Paula Malo De Molina1,4
Successful control of the protein collapse by varying solvent conditions and crosslinker lengths:
The higher urea concentration leads to larger precursor chain expansion.
The longer the crosslinker, the easier the loop formation along the chain → better collapse.
→ Our results show that the precursor chain conformation has an impact on the BSA-SCNP microstructure.
CONCLUSION
: radius of gyration
scaling exponent
  1/3  globule.
  0.5  conformation of a linear polymer chain in θ-conditions.
  0.6  swollen chain in a good solvent (self-avoiding-walk conformation).
  Single chain nanoparticles (SCNPs) are unimolecular polymer chains folded or collapsed via intra-molecular cross-linking under high dilution, leading to sparse conformations and a topological polydispersity similar
  to that of intrinsically disordered proteins (IDPs). To extend SCNPs to polypeptides for biocompatibility purposes, it is important to understand the role of the chain conformation of the
  precursor on the resulting SCNP morphology. For this, we have systematically varied the solvent conditions (pH and denaturant concentrations) of BSA solutions as well as the crosslinker (lengths and concentrations) and studied the resulting SCNPs by scattering techniques.
METHODOLOGY
SANS
DLS/SLS
The higher urea concentration leads to larger precursor chain expansion (↑, ↑ ).
pH has only a small effect.
θ
Structural control by solvent conditions
pH=7.4
BSA CONFORMATION
SCNP FORMATION
Greater chain collapse (↓, ↓) with the addition of crosslinker for higher urea concentrations.
No significant effect of pH.
1 Materials Physics Center (CSIC–UPV/EHU) San Sebastián, Spain.
2 ISIS Neutron and Muon source, Rutherford Appleton Laboratory, England.
3 Donostia International Physics Center, San Sebastián, Spain.
4 IKERBASQUE – Basque Foundation for Science, Bilbao, Spain.
INTRODUCTION
long crosslinker – BS3
short crosslinker - DSG
pH=8.2
pH=8.2
pH=7.4
pH=8.2
pH=7.4
Native BSA (0M Urea): Ellipsoid fit
Guinier approximation to estimate
Denatured BSA: Generalized Gaussian coil expression
where
.
No aggregation at much lower Q → mainly intra-molecular cross-linking.
↓ with additional crosslinker concentration.
Long crosslinker
pH 7.4
pH 8.2
[urea] = 5.4M
[urea] = 6.3M
[urea] = 7.2M
1) Influence of the solvent conditions
7.2M urea, pH 7.4, long crosslinker
3) Effect of the crosslinker length
Longer crosslinker is more effective in chain compaction.
@7.2M urea
Paula Malo de Molina, Thu Phuong Le, Amaia Iturrospe, Urs Gasser, Arantxa Arbe, Juan Colmenero, and José A. Pomposo, ACS Omega 2022 7 (46), 42163-42169
Fitting parameters to a generalized Gaussian coil
SANS
SLS
DLS
2) Complementary light scattering measurements
Long crosslinker
Short crosslinker
%cross-linker
% cross-linker
Θ=100˚